Logo

Description automatically generated

**Canson Infinity Baryta Prestige II**

|  |  |
| --- | --- |
| **Weight (gsm)** | 340 |
| **Thickness (µm)** | 400 |
| **Surface feel** | Smooth |
| **Surface finish** | Gloss |
| **Composition** | Alpha-cellulose and cotton |
| **CIE Whiteness** | 88 |
| **Acid free paper** | Yes |
| **OBA content** | No |
| **Drying time** | Immediate |
| **Water resistance** | High |
| **ISO 2471 Opacity** | >99 |
| **Internally buffered** | Yes |
| **Additional comments** | Optimised for Pigment and Dye Inks  ISO 9706  FSC Certified |